## Slide 1
Photo by Stefan Els
Practical 3: Elements to Minerals Conversion

## Slide 2: Outcomes
Slide 2
The outcomes of this topic include:
  Identify the primary minerals associated with specific elements in ore samples.
  Relate elemental assay data to mineralogical composition.
  Convert elemental concentrations (from XRF, ICP-MS, or other techniques) into mineral abundances.
  Use stoichiometric calculations to estimate mineral proportions.
  Understand the limitations of element-to-mineral conversions based on analytical uncertainties.
Notes: Image sources, check all slide numbers throughout.

## Slide 3: Elements to Minerals Conversion
For simple ores comprising only one or two valuable minerals associated with a diagnostic element, the mineral grades can be calculated from known mineral compositions (measured using EPMA ) or from stoichiometric mineral compositions.
A × X = b
    A represents the fraction of element in the mineral,
    X is the wt.% of the mineral in the sample (mineral grade)
    b is the wt.% of the element in the sample (element grade).
This approach however relies on prior knowledge of which valuable minerals are present and although elegant, should be handled with care

## Slide 4
Photo by Stefan Els
Practical 3: Elements to Minerals Conversion
Example

## Slide 5: Elements to Mineral Conversion - Example
Slide 2
We process minerals and not metals …
Given that a sulphide ore composed of the following minerals and elemental composition/grade assays (Weight %) :
🔸 What is the percent of bornite, millerite, and pyrite in the ore? Practical 3_Example and Exercise_Final
Element | Wt. % | Molar Mass (g.mol-1)
Cu | 2.10 | 63.55
Ni | 2.75 | 58.70
Fe | 60.30 | 55.85
S | 34.85 | 32.07
Mineral | Formula
Bornite | Cu5FeS4
Millerite | NiS
Pyrite | FeS2
Notes: Image sources, check all slide numbers throughout.

## Slide 6
Photo by Stefan Els
Practical 3: Elements to Minerals Conversion
Exercise

## Slide 7: Elements to Mineral Conversion - Exercise
Slide 2
Following the characterization of an ore a simplified version of the assay data is presented in Table 1. The mineralogical data is presented in Table 2. Based on this data, calculate the percentage of each mineral in the ore sample.
Element | Chemical assay (Wt. %) | Molar Mass (g.mol-1)
Si | 9,72 | 28,09
Fe | 18,89 | 55,85
S | 22,33 | 32,07
Cu | 11,76 | 63,55
Zn | 5,98 | 65,39
Pb | 8,72 | 207,2
Ba | 6,67 | 137,33
Mineral | Formula | Molar mass (g/mol)
Chalcopyrite | CuFeS2 | 183,52
Galena | PbS | 239,27
Sphalerite | ZnS | 97,46
Barite | BaSO4 | 233,39
Pyrite | FeS2 | 119,98
Magnetite | Fe2O3 | 159,69
Quartz | SiO2 | 60,08
Table 1: Chemical assay data of the ore sample.
Table 2: Mineralogical data of the ore sample.
Notes: Image sources, check all slide numbers throughout.

## Slide 8: Thank you!
Photo by Stefan Els
Notes: Thank you for listening.